## Slide 1: Progress in Active Infrared Imaging for Defect Detection in the Renewable and Electronic Industries
Presenter: Jung Wook

## Slide 2: 目录
01
Introduction
02
Key Techniques
03
Renewable Industry
04
Electronic Industry

## Slide 3: Introduction
01

## Slide 4: 1.Introduction
Electromagnetic waves
Any object in nature that is above absolute temperature (−273 ◦C) radiates heat
(electromagnetic waves) outward
Infrared：a wavelength range of
760 nm to 1 mm
The higher the
temperature of an object, the greater the energy radiated

## Slide 5: Principle of infrared thermal imaging (IRT) technology
05
04
03
02
01
The object
Optical grating
Infrared chart
Lens
Detector

## Slide 6: Advantages of IRT technology
01
Non-contact and non-invasive
04
The observation results can directly reflect the problem
Intuitive and easy-to-understand results
02
Fast moving objects can be continuously detected.
High-speed
03
Can be used over and over again for the same target.
Relatively safe
Test the stability of hazardous materials.

## Slide 7: Prospects for development
This upward trend suggests the increasing significance of IRT across various academic disciplines, motivating researchers to delve deeper into the applications and advancements of IRT technology.
This is distinctly demonstrated in the chart, providing robust support and impetus for current and future IRT research.
The citation frequency and number of publications for the keyword “IRT” were searched for in Web of Science
Chart: 图表标题
| 类别 1 | 类别 2 | 类别 3 | 类别 4
系列 1 | 4.3 | 2.5 | 3.5 | 4.5
系列 2 | 2.4 | 4.4 | 1.8 | 2.8
系列 3 | 2 | 2 | 3 | 5

## Slide 8: Key Techniques
02

## Slide 9: 2.1 PT AND LT
Infrared Camera→A thermal pulse is emitted to the sample→
Fast infrared camera records images→
The computer uses algorithms to create images
Schematic of PT tests in the defect detection process
The signal generator generates heat waves→
The infrared camera captures the thermal reaction of the sample→
The analysis results determine the defect location.
Schematic of LT tests in the defect detection process

## Slide 10: 2.2 UVT AND ECT
The ultrasonic transducer excites the specimen to be detected→
The vibration propagates inside the material, leading to localized heating of cracks through internal friction→
Infrared cameras capture temperature changes
Schematic of UVT tests in in the defect detection process
A coil with pulsed excitation is brought near the test specimen→
Induced eddy currents surround defects or impurities→
Form temperature field distribution
Schematic of ECT tests in in the defect detection process

## Slide 11: 2.3 Classification of thermal imaging techniques
2.3.1 Transient heat transfer
The Fourier diffusion equation
The one-dimensional heat flow of Equation
Transient heat transfer
↓
↓
Steady-state heat conduction :
The temperature at each point in the heat transfer process does not change with time, and the heat transfer rate is independent of time.
The heat flow rate remains constant

## Slide 12: 2.3 Classification of thermal imaging techniques
2.3.2 Static heat transfer
Transient heat conduction :
The temperature of each point in the heat transfer process changes with time, and the heat transfer rate is not constant.
𝜔 is the modulated frequency,
𝜆 corresponds to thermal wavelength,
𝑇0 is the initial temperature,
𝜇 is expressed as thermal diffusion length
An isotropic semi-infinite specimen

## Slide 13: Renewable Industry
03

## Slide 14: 3.1 Photovoltaic solar
1.Old:
Traditional electrical performance testing of PV modules is a mature testing method, but it has limited fault-detection capabilities.
2.New:
Using IRT methods
Detection Method

## Slide 15: 3.2 Optical Degradation
1. Causes Of PV Optical Degradation
(1) Water infiltration in the environment causes changes in the structure of the pv panel.
(2) Faulty cells result in mismatch losses, thereby leading to an uneven distribution of cell temperature (Tc) across the PV module.
2. PV Module In The Field:
(a) under environmental stressors e.g., high humidity, temperature, and UV radiation, moisture can enter the PV module ;
(b) IRT characteristics of PV Module X acquired under clear sky outdoor conditions;
(c–e) EL characteristics acquired under Isc bias conditions of the corresponding marked areas in (b) .
Optical Degradation In PV

## Slide 16: 3.3 Electrical Mismatches and Degradation
1. Fault types :
Cell cracks, snail trails, broken interconnecting ribbons and busbars, shunts, and poor soldering.
2. Methods of diagnosing faults :
The measurement of Current–Voltage (I–V) characteristics.
3. PV module in the field:
(a) typical I–V characteristic output . IRT of an electrically mismatched PV module, due to broken interconnection ribbons;
(b) defective soldering/busbar
(c),(d) thermal image of PV module
Electrical Mismatches And Degradation In PV

## Slide 17: 3.4 Non-Classified Faults
(a) thermal images taken by operators using standard lenses ;
(b) the thermographic image was captured at an angle that is not perpendicular to the module ;
(c) thermal image obtained by standard lens ;
(d) thermal image obtained by wide-angle lens ;
(e) host spot profiles variation for different examined PV module defects.
Potential-induced degradation (PID) and defective bypass diodes

## Slide 18: 3.5 Summary
Future defect detection technology :
The thermal image is preprocessed
↓
Using deep learning models
↓
Extract features related to defects
↓
Automatic analysis of results

## Slide 19: Electronic Industry
04

## Slide 20: 4.1 Intruduction
1. Primary territories
Semiconductor wafer production：
Chip，PCBs，Weld，Others.
2.Application purpose
Narrow and reduce production defects.
Development of IRT in the field of electronics

## Slide 21: 4.2 Chip
Schematic representations of two distinct laser-based thermographic inspection methods:
(a) line laser lock-in thermography system
(b) corresponding thermograms of vertically oriented crack chips and horizontally oriented crack chips within this system ；
(c) multi-point laser lock-in thermography system ；
(d) corresponding thermograms of vertically oriented crack chips and horizontally oriented crack chips within this system].

## Slide 22: 4.3 PCBs
IRT in PCBs :
(a) 2D and 3D views of transient amplitude images ;
(b) amplitude and phase images in lock-in thermography ;
(c) defective and non-defective reference regions

## Slide 23: 4.4 Weld
Schematic diagram of welding defect detection: types of weld defects：
(a) ,(b) schematic of experimental setup and distribution of welds in test samples ;
(c) experimental setup and distribution diagram;
(d) infrared thermal images of weld defects

## Slide 24: Outlooks
05

## Slide 25: Future development
Improvements in PV panels
Widespread adoption in electronics manufacturing
Seamless integration with AI

## Slide 26: THANKS
Presenter: Jung Wook